MTSE 3080 Materials Processing Syllabus, Spring 2010

Instructor:                  	Rick Reidy

Office Hours:             	3:00 PM to 4:00PM, MW

Office Location:        	E108 Discovery Park

Phone:                        	940-36-7115                                     Email: reidy@unt.edu

Course Meeting Time:  	9-10:20pm TTH

Course Meeting Location: 	D207B Discovery Park

Course assignments: 2 exams (30% each), 3 homeworks (10%), and 1 final (30%)

| Date | Topic | Date | Topic |
| --- | --- | --- | --- |
| Jan 19 | Intro, Ceramic Processing | Mar 4 | Polymer synthesis |
| Jan 21 | powder synthesis, Sol-Gel synthesis | Mar 9 | Polymer melt processing |
| Jan 26 | Ceramics high temperature processing | Mar 11 | Polymer processing |
| Jan 28 | Glass processing | Mar 23 | SECOND EXAM |
| Feb 2 | Ceramic densification | Mar 25 | Polymer processing |
| Feb 4 | Metal processing | Mar 30 | Polymer processing |
| Feb 9 | Metal separation, hydrometallurgy | Apr 1 | Composites |
| Feb 11 | Pyrometallurgy | Apr 6 | No class |
| Feb 16 | First Exam | Apr 8 | introduction, electronic materials, Silicon |
| Feb 17 | Powder metal processing | Apr 13 | IC construction |
| Feb 23 | High temperature metal processing | Apr 15 | thin films-- film deposition, metal, dielectrics |
| Feb 25 | Metal heat treatment, phase transformations | Apr 20, 22 | Wet processes |
| Mar 2 | Metal hardening and strengthening | Apr 27, May 4 | Plasma processing |
| May 6 | Review | May 11 | FINAL EXAM (comprehensive) |

- Attendance is expected for each class.  If you are unable to make a class, please let me know so that I don’t wait for you.

- Difficulties with exam dates must be addressed by the Friday before the assigned date.

- Although this schedule is quite full, additional topics may be added in response to class interest.

- If applicable, grades will be assigned by natural breaks in the score distribution.  If this method is inconclusive, the median will be used to separate A’s and B’s.

- The University of North Texas Materials Science Department will make reasonable adjustments to ensure equal opportunity for qualified persons with disabilities to participate in all of their programs and activities.  Please see the instructor if special accommodations are required.